## Slide 1: Dimensionality Reduction Methods for Spectral Analysis
Sergei V. Kalinin

## Slide 2: Linear Unmixing methods
Why linear unmixing?
  Spectral images
  Image analysis
Multiple linear regression
Principal component analysis (PCA)
  Definition and implementation
  PCA for scanning tunneling microscopy
  Physical meaning of PCA: band excitation SPM
  PCA on imaging data
Independent component analysis (ICA)
N-FINDR and Bayesian linear unmixing
  Mapping phase transitions
  Image segmentation
Physical constraints in linear models: If solution exists and its unique, doesn’t matter how you find it
Notes: For recording – remove figures

## Slide 3: Spectroscopic Imaging
Scanning probe microscopy:
Force-distance curve measurements
Current-voltage measurements
Piezoresponse force/electrochemical strain spectroscopy
Advancements in imaging led to a broad spectrum of the spectroscopic imaging techniques, in which response spectra are measured in each spatial location giving rise to 3- and higher dimensional data.
Electron microscopy:
Electron Energy Loss Spectroscopy
Optical microscopy:
Hyperspectral imaging
Time resolved measurements
Mass-spectrometry:
Secondary ion MS imaging
In many cases, measured signal can be represented or approximated as a linear combination of signals. However, their functional forms are generally unknown
Very important: convolution with resolution function is also mixing
Figure by S. Jesse

## Slide 4: Less obvious cases
1. Ptychography in STEM
electron beam
Specimen
Sub-Å probe
Advanced
DAQ
Direct
Electron
Detection
To scan control coils
3. Image analytics
Collected is diffraction pattern (ronchigram) in each location
2. Focussed X-Ray
Sliding image transforms:
Fast Fourier Transforms
Correlation functions
Intensity histograms
Structural descriptors
The M pixel 2D image is transformed to M/N pixel image of more complex structure
N
Collected is diffraction pattern in each spatial location in 2D or 3D
Figure by M. Ziatdinov
Notes: Please ask Alex Belianinov about image

## Slide 5: Physics vs. ML based analysis
Physical model
Machine learning
If we have physical model, we can extract relevant parameters from data
Model can be imperfect – epistemic uncertainty
Data can be noisy – aleatoric uncertainty
Analysis results do not depend on sampling of data
If we don’t have physical model, we can learn intrinsic structure of data
Unsupervised learning: based on data only
  But not really (definition of distance)
  Analysis results can depend on sampling of data
Supervised learning: based on examples of prior data
  Out of distribution shifts
  Analysis does not affect on sampling of the data
Physics-informed ML: Combines strengths (and limitations) of both approaches

## Slide 6: General linear unmixing
+N
We start with:
x is the spatial variable, x = (x,y)
R is the (vector) parameter variable
Overall, for MxM image and P point in spectra, we have M2P data points
We aim to get:
are loading maps
are endmembers/eigenvectors
N is noise
Overall, we can have (maximum) P loading maps of M2 size. However, not all of them will have useful information
R
wi
Figure by S. Jesse

## Slide 7: Multiple Linear Regression
+N
STEM of STO/LSMO/BFO interface
Low-loss EELS spectra of three components
χ2 map
Fit coefficient map
residuals map
“Chemistry”:
35 to 125 eV
“Plasmons”:
5 to 35 eV
but are known
Linear mixing
Standard spectra
A.Y. Borisevich et al, Suppression of Octahedral Tilts and Associated Changes in Electronic Properties at Epitaxial Oxide Heterostructure Interfaces, Phys. Rev. Lett. 105, 087204 (2010).

## Slide 8: But what if endmembers are unknown?
At the first glance, the problem is impossible. We want to separate mixture in the components without knowing what the components are!
What we can do:
Principal component analysis: how many components are there in the mixture
Independent component analysis: going against the law of big numbers
Bayesian linear unmixing: additivity to 1 and non-negativity constrains
What can be done:
Bayesian linear unmixing: constraints on endmembers
Sparse reconstructions: small number of components in each point
Constraints on loading maps: smoothness or sharp boundaries
Kernel transforms: data is simplest if physics is correct
Notes: Need to change images – likely copyrighted

## Slide 9: Principal Component Analysis
In PCA, the eigenvectors are orthonormal and are arranged such that corresponding eigenvalues are placed in descending order by variance
Can be used to separate “real data” from “noise” – but needs cut-off/selection criteria
Can be performed by SVD decomposition (MatLab, Python, etc)
PCA eigenvectors do not have defined physical meaning
However, PCA is a starting point for many other unmixing methods

## Slide 10: PCA Background
PCA: orthogonal transformation converting possibly correlated variables into linearly uncorrelated principal components
PCA was invented by Karl Pearson in 1901, however the Singular Value Decomposition was independently derived some half a century earlier in Italy, Germany and France
PCA transforms the data such that the greatest variance by any projection lies on the first coordinate
Reveals internal structure of the data that best explains variance in the data set
Since data often moves in clusters, PCA reveals those variables that drive the variance
Pearson, K. (1901). "On Lines and Planes of Closest Fit to Systems of Points is Space". Philosophical Magazine Series 6 2 (11): 559–572

## Slide 11: PCA: Formal Definition
Principal component w1 of a data set X can be defined as:
Subsequent components k, can be found by simply subtracting k-1 components from the data
And substituting as Ẋk-1 a new data set

## Slide 12: PCA in Python…
… is really simple – we will see in the Colab. However, it is important to understand what is that we are doing!

## Slide 13: PCA: outside of imaging
Spectroscopic, or any type of series data becomes superposition of orthogonal eigenvectors with different weights
First eigenvector contains the most information within spectral dataset
Second eigenvector contains the most common response after subtraction of the 1st etc.
Great, quick tool for looking at multichannel data
Dan Alcantra, Localized Components Analysis, http://idav.ucdavis.edu/~dfalcant/research/loca.php
D. Alcantara, O. Carmichael, E. Delson, W. Harcourt-Smith, K. Sterner, S. Frost, R. Dutton, P. Thompson, H. Aizenstein, O. Lopez, J. Becker, and N. Amenta, "Localized Components Analysis", Proceedings of IPMI, 2007, pp. 519 - 531

## Slide 14
Why should we look at the historical papers:
Often contain elementary introductions
Deep insights into principles
Surprisingly prescient predictions
Comparison with the present: see th ebig picture
““Those who cannot remember the past are condemned to repeat it.”
George Santayana,
The Life of Reason, 1905

## Slide 15
Why did the PCA on EELS started to grow in 2005 – 2010?

## Slide 16: Grain boundary by STM
3.6 nm
-106pm
1.4 nm
72pm
Voltage (V)
-0.5V
0.5V
Pixel
1
10
1.4
1
0.4
4
Topographical STM of FeSeTe, T = 82K 15x15nm2, 50mV, 100pA, white rectangle represents area where CITS was performed; (b) CITS 80x80 pixel graphical average of the spectrographic data.
M. Ziatdinov, A. Maksov, L. Li, A. Sefat, P. Maksymovych, and S.V. Kalinin, Deep data mining in a real space: Separation of intertwined electronic responses in a lightly-doped BaFe2As2, Nanotechnology 27, 475706 (2016).

## Slide 17: Eigenvectors and loadings
Figure by A. Belianinov

## Slide 18: Scree plot and correlations
Semi log plot indicating the “weight” of each component as a function of all components
Only the first few components contain useful info, while others are dominated by noise
Spatial correlations
PCA Eigenvectors
For AFM data
We can also analyze correlations in images
Figure by A. Belianinov

## Slide 19
Comparison: PCA vs. functional fit
Band excitation scanning probe microscopy
Signal formation mechanism: simple harmonic oscillator

## Slide 20: Comparison: PCA vs. functional fit
PC1
PC2
PC3
Amplitude
Frequency
Q
4 hrs
0.4 sec
S. Jesse and S.V. Kalinin, Principal component and spatial correlation analysis of spectroscopic imaging data in scanning probe microscopy, Nanotechnology 20, 085714 (2009).

## Slide 21: When does PCA match physics?
Simulate simple harmonic oscillator curves for different variations of resonance frequency and noise levels
There is similarity between variational derivatives of SHO responses and PCA eigenvectors
S. Jesse and S.V. Kalinin, Principal component and spatial correlation analysis of spectroscopic imaging data in scanning probe microscopy, Nanotechnology 20, 085714 (2009).

## Slide 22: K-mean clustering
PCA is decomposition. But sometimes, we don’t want to decompose our signal, but just group them into ‘alike’ sets.
This is termed ‘clustering’. The easiest and most widely used method is the k-means algorithm
(Determine S = {S1,S2,…Sk}, such that within cluster sum of squares is minimized)
K-means Clustering algorithm, to separate data (x1,x2,…,xn) into k clusters
where µi is the mean of points in Si
Step 1
Step 2
Step 3
Step 4
Source: Wikipedia

## Slide 23: K-means clustering
K-means result of the CITS map broken into
three distinct clusters: CITS map of all three clusters combined vs. individual cluster distribution in the map
M. Ziatdinov, A. Maksov, L. Li, A. Sefat, P. Maksymovych, and S.V. Kalinin, Deep data mining in a real space: Separation of intertwined electronic responses in a lightly-doped BaFe2As2, Nanotechnology 27, 475706 (2016).

## Slide 24: Independent Component Analysis
PCA: orthogonal transformation of possibly correlated variable into a set of linearly uncorrelated variables
    Analyzes data representing observations described by dependent variables which are inter-correlated
    Main goal is to find true variables assuming that corrupting noise is Gaussian
ICA” method for separating multivariate signal into additive subcomponents assuming statistical independence of source signals
    Finds components that are maximally independent and non-Gaussian
    Blind source separation – cocktail party problem
Compared to PCA, ICA can produce statistically independent non-Gaussian components by decorrelating the higher-order moments in addition to the first- and second-order moments of the statistical distribution

## Slide 25: Mathematics of ICA
Data as a set of vectors
Components of the data
The Goal is to transform observed data into maximally independent components measured
through some function of independence.
An observed data vector x can then be represented as a sum of independent components s
weighted by some mixing weight a:
or
In other words, our data vector x is represented by basis vectors
that can form columns of a mixing matrix such that:
https://en.wikipedia.org/wiki/Independent_component_analysis

## Slide 26: Mathematics of ICA - 2
Given that our data is set of vectors x, we want to find both, the mixing matrix A and sources s
This can be done by calculating w vectors and a cost function that can maximize the
Non-Gaussianity, or minimize mutual information of
Original sources can then be recovered by multiplying observed data vectors x with the
inverse of the mixing matrix:
Not as easy to utilize as PCA, but excellent premade algorithms are readily available:
Aapo Hyvärinen – FastICA*
RIKEN developed – ICALAB Toolbox
Bell-Sejnowski, Molgedey-Schuster – ICA Toolbox
http://cis.legacy.ics.tkk.fi/aapo/papers/IJCNN99_tutorialweb/IJCNN99_tutorial3.html
http://research.ics.aalto.fi/ica/fastica/

## Slide 27: Cocktail Party Problem
Notes: Ask Alex

## Slide 28: ICA Example
Sources
Observations
PCA Components
ICA Components
Components are maximally independent

## Slide 29: Bayesian Linear Unmixing
+N
The eigenvectors are non-negative, ≥0
The loading coefficients sum to 1
The number of eigenvectors, K, is a priori unknown
BLU is ideally suited for certain classes of problems, e.g. conduction through parallel channels, optical or electronic spectra of mixtures, etc

## Slide 30: Dobigeon BLU
Nicolas Dobigeon, Saïd Moussaoui, Martial Coulon, Jean-Yves Tourneret, Alfred O. Hero; IEEE TRANSACTIONS ON SIGNAL PROCESSING, VOL. 57, NO. 11, NOVEMBER 2009
Dobigeon presents a Bayesian with a MCMC Gibbs sampler for estimating endmember spectra and its relative abundance in a spectral image
Y = MA + N
Where Y is the noisy observation comprised of endMembers with corresponding Abundances corrupted by additive Gaussian Noise
This algorithm proposes to estimate the initial projection of endmembers in a dimensionality reduced subspace (PCA) via N-FINDR that finds simplex of maximum volume that can be inscribed within the hyperspectral data set using a simple non-linear inversion
Endmember Abundance priors as well as Noise variance priors are chosen by a multivariate Gaussian distribution (this is a nontrivial assumption that rests in computational implementation)
Posterior Distribution is calculated based on endmember independence using Markov Chain Monte Carlo that generates asymptotically distributed samples probed by Gibbs sampling strategy

## Slide 31: Laser heating induced phase transitions
Copper indium thiophosphate (Cu0.77In1.12P2S6) layered ferroelectric
  Ferroelectric state at room temperature
  Curie temperature Tc = 320 K
  Non-polar In4/3P2S6 inclusions
Combined Atomic Force Microscopy (AFM) and confocal Raman spectroscopy investigative approach
  AFM – topography measurements
  Piezoresponse force microscopy (PFM) – static ferroelectric domain structure
  Raman – crystallographic structure via Raman spectra
Ferroelectric domain structure
PFM amplitude
PFM phase
Experimental scheme
Single point Raman spectra
A. Ievlev, ACS Nano 9, 12442 (2015).

## Slide 32: Laser heating induced phase transition
Laser can be used for local heating to induce ferroelectric- paraelectric phase transition
Measurements with variation of the laser power
  PFM – in-situ change in the domain structure above Tc
  Raman – evolution of the Raman spectra through the phase transition
Comprehensive analysis of Raman spectra is complicated by inhomogeneous chemical composition and high noise level
Bayesian Linear Unmixing can be used for automated identification of spectra evolution
PFM amplitude
PFM phase
Raman spectra evolution (averaged)
Domain structure evolution
Laser power
A. Ievlev, ACS Nano 9, 12442 (2015).

## Slide 33: BLU separation of components
Results of BLU: components and loading maps
Spatial concentration of components
Phase transition
Unmixing showed presence of three independent components (contributions into Raman spectra):
  Non-polar In4/3P2S6 – weak changes in intensity with temperature
  Paraelectric CuInP2S6 above Tc – appears at higher laser powers
  Ferroelectric CuInP2S6 below Tc – disappears at higher temperatures
A. Ievlev, ACS Nano 9, 12442 (2015).

## Slide 34: First order reversal curve IV measurements
First order reversal curves in IV measurements
Opening of hysteresis loops indicates onset of slow-bias-induced changes
These can be explored as a function of rate and bias

## Slide 35: Conductance in nanotubular structures
BFO matrix
CFO
Topography
Current Map
Topography
Current Map
Current Map
Current Map
Probing electrochemistry through electronic degrees of freedom
Y.H. Hsieh, E. Strelcov, J.M. Liou, C.Y. Shen, Y.C. Chen, S.V. Kalinin, and Y.H. Chu, Electrical Modulation of the Local Conduction at Oxide Tubular Interfaces, ACS Nano 7, 8627 (2013).

## Slide 36: FORC IV of BFO-CFO
Current map @ 0.1 V
Topography
Current maps
FORC-IV Loop area maps
Clear variability of conductance and loop opening behavior
“Too much data” – FORC IV loops that can be reduced to multiple current and loop opening maps as a function of peak voltage
E. Strelcov et al, ACS Nano 8, 6449 (2014).
Averaged IV’s
Notes: E. Strelcov, A. Belianinov, Y.H. Hsieh, S. Jesse, A.P. Baddorf, Y.H. Chu, and S.V. Kalinin, Deep Data Analysis of Conductive Phenomena on Complex Oxide Interfaces: Physics from Data Mining, ACS Nano 8, 6449 (2014).

## Slide 37: Bayesian linear unmixing
Endmembers
Loading Maps
Ohmic
Non-linear
Low conductivity
Memristive
Separates 4 different types of behavior, all making physical sense. Loading maps normalized to unity.
BEI1
BEI2
BEI3
BEI4
E. Strelcov, A. Belianinov, Y.H. Hsieh, S. Jesse, A.P. Baddorf, Y.H. Chu, and S.V. Kalinin, Deep Data Analysis of Conductive Phenomena on Complex Oxide Interfaces: Physics from Data Mining, ACS Nano 8, 6449 (2014).
Notes: E. Strelcov, A. Belianinov, Y.H. Hsieh, S. Jesse, A.P. Baddorf, Y.H. Chu, and S.V. Kalinin, Deep Data Analysis of Conductive Phenomena on Complex Oxide Interfaces: Physics from Data Mining, ACS Nano 8, 6449 (2014).

## Slide 38: Fit to physical models
BEI2 to FN
BEI4 to PF
BEI4 to FN
BEI3 to FN
Fowler-
Nordheim
Schottky
Poole-
Frenkel
Mott-
Gurney
Child’s
Law
Mechanism\
Endmember
E. Strelcov, A. Belianinov, Y.H. Hsieh, S. Jesse, A.P. Baddorf, Y.H. Chu, and S.V. Kalinin, Deep Data Analysis of Conductive Phenomena on Complex Oxide Interfaces: Physics from Data Mining, ACS Nano 8, 6449 (2014).
Notes: E. Strelcov, A. Belianinov, Y.H. Hsieh, S. Jesse, A.P. Baddorf, Y.H. Chu, and S.V. Kalinin, Deep Data Analysis of Conductive Phenomena on Complex Oxide Interfaces: Physics from Data Mining, ACS Nano 8, 6449 (2014).

## Slide 39: FORC IV workflow

## Slide 40: Wait, there is more!
We need un-mixing/decomposition that are infused in some universal manner with a priori physical information (trivial example is constraints, a less trivial one is a simulation of some expected components) so that the resultant components can be directly interpreted in physical terms.
For example:
Bayesian linear unmixing: constraints on endmembers
Sparse reconstructions: small number of components in each point
Constraints on loading maps: smoothness or sharp boundaries
Kernel transforms: data is simplest if physics is correct